# ÖZ

Bu çalışmada sığır karbonik anhidraz enziminin (BCA) alginat doğal polimerinin CaCl2 ile oluşturduğu kalsiyum alginat mikro küreleri üzerine immobilizasyonu araştırıldı. İmmobilizasyon için en uygun alginat ve CaCl2 derişimleri optimize edildi. İmmobilize enzimin immobilizasyon verimi ve aktivite verimi tespit edildi. İmmobilize enzimin kinetik parametreleri (Vmax, Km), optimum sıcaklığı, optimum pH’ı tespit edilerek serbest enziminki ile karşılaştırıldı. Molekül ağırlığının immobilizasyon üzerine etkisinin araştırılması için pazı (Rumex patientia L.) bitkisinden elde edilen özütünün (PCA) aynı koşullarda immobilizasyonu gerçekleştirildi ve kinetik parametreleri BCA’ın kinetik parametreleri ile karşılaştırıldı. BCA ve PCA’ın polimer matrikse bağlandığı termal analiz yöntemleri ile gösterildi.

# ABSTRACT

In this work, immobilization of bovine carbonic anhydrase (BCA) on calcium alginate beads obtained by CaCl2 and alginate natural polymer.

Optimization of alginate and CaCl2 concentrations as well as immobilization yield and activity yield are calculated. Kinetic parameters (Vmax, Km) and optimum temperature and pH values of the immobilized enzyme are determined and compared to the parameters that of free enzyme. In order to investigate the effect of molecular weight to the immobilization yield CA crude extract obtained from patience dock (Rumex patientia L.) leaves (PCA) immobilized to alginate beads under the same conditions and kinetic parameters are compared to the immobilized BCA. İmmobilization of BCA and PCA to alginate beads is demonstrated via thermal analysis methods.

ANAHTAR SÖZCÜKLER / KEY WORDS : Sığır karbonik anhidraz, Bitki karbonik anhidraz, İmmobilizasyon, Alginat, Kinetik parametreler / Bovine carbonic anhydrase, Plant carbonic anhydrase, Immobilization, Alginate, Kinetic parameters.